**Engineering Question**

**Question 1:**  The PCB board fabrication information is not specified.

**Suggestion :** Follow below information to make this board, unless otherwise specified.

Material: FR-4 TG≥150.

Finished board thickness shall be 1.6mm+/-10%.

Finished copper thickness shall be 35um on both outer layers and 35um base copper in inner layers.

Black color of solder mask.

White color of silkscreen

Surface finish shall be HASL-lead free.

